## Slide 1
Internship presentation 10-08-2022
Y. Baron Supervisors: J.E. Scheerder, P.M. Koenraad, C. Fleischmann
Interface characterization in SiGe/Si/SiGe multilayers
using atom probe tomography

## Slide 2: Introduction
Si is promising for development of qubits:
  Well established fabrication and research
  Zero nuclear spin → long spin lifetime
  Qubit performance dependent on SiGe/Si interfaces
Final goal: characterize the buried interfaces using APT and link the results to the qubit performance
  Determine influence of different fabrication conditions
Project goal: Evaluate the reliability of APT for interface characterization
F.A. Zwanenburg et al., Silicon Quantum Electronics, Rev. Mod. Phys. 85, 961 (2013)
public

## Slide 3: Atom Probe Tomography: Step-by-step
ROI
Sample preparation
  Relies on controlled field evaporation
  Can measure in voltage or laser pulse mode
  Hit position and sequence is recorded
  Time of flight is used to identify chemical species
Data acquisition
Image adapted from M.Dialameh Ph.D. dissertation (2019)
public
public

## Slide 4: Atom Probe Tomography: Step-by-step
Chemical identification
Tomographic reconstruction
  Peaks can then be identified
  Simplified reconstruction protocol:
    Field evaporation assumed from a hemispherical shell
    Assumes sequence of evaporation is well controlled
  Uses certain static reconstruction parameters
    Detection efficiency
    Image compression factor
reconstruction
public
public
Image adapted from B. Gault at al. Atom Probe Microscopy, Springer New York, vol. 160 (2012)

## Slide 5: Atom Probe Tomography: Step-by-step
  Define cubical ROI 10x10x30 nm
  Find transition width by fitting sigmoid function to concentration profile:
  Find 15 at% Ge isosurface and calculate mean and rms roughness using Gwyddion
Isosurfaces
Interface characterization
public
public

## Slide 6: Contents
Reconstruction calibration (crystallography)
Identify and correct artifacts in reconstruction
Deviations while varying the ICF
Conclusion and outlook
public
public

## Slide 7: Reconstruction calibration
Use geometric information to calibrate reconstruction:
  Si layer thickness
  Curvature of interfaces
  Crystallography?
Ge ~ 30 at%
Ge ~ 30 at%
ICF = 1.2
ICF = 1.8
public
public
C. Kittel, Introduction to solid state physics, John Wiley & Sons. (2004)

## Slide 8: Reconstruction calibration: crystallography
Crystallographic information in APT data
  Detector event histogram
  Spatial Distribution Maps
Not all information on crystal structure is immediately visible:
  needs extra filtering → first try on Sb-doped Si sample
Ge ~ 30 at%
Ge ~ 30 at%
public
public

## Slide 9: Reconstruction calibration: crystallography
Number of pulses before evaporation is lower in pole regions*
→ filter for hits where
1.
2.
2.
1.
public
public
* L. Yao, MethodsX, vol. 3, pp. 268–273 (2016), DOI:10.1016/j.mex.2016.03.012
Notes: Say that DR is typically <1%

## Slide 10: Reconstruction calibration: crystallography
public
Direction | Theoretical lattice spacing
<400> | 0.136 nm
<311> | 0.161 nm

## Slide 11: Reconstruction calibration: crystallography
Silicon
SiGe/Si/SiGe
Crystallography can be used in doped Si, but not in SiGe/Si/SiGe multilayer
→ use Si layer thickness and interface curvature
public
public

## Slide 12: Identify and correct artifacts in reconstruction
Expected artifacts (related to different evaporation fields of Si and Ge):
  Artificial density fluctuations
  Curvature of SiGe/Si interfaces
Measure sample in two directions:
  Interface characterization should be independent of direction
Evap.
dir.
Top-down
Evap.
dir.
Backside
public
public

## Slide 13: Identify and correct artifacts in reconstruction
Clear density fluctuations observed
Low/high density interface depends on evaporation direction
Solution: apply a density correction
public
public

## Slide 14: Evaluate influence artifacts on interface characterization
public
public
Low density → larger transition width
High density → smaller transition width
Density correction reduces influence evaporation direction
High density
interface
Low density
interface

## Slide 15: Deviations while varying the ICF
Dependence visible in isosurface
Top and bottom interface are flat for different values of the ICF
Shift induced after density correction and Si layer thickness is reduced
Similar behaviour observed in both evaporation directions (though top/bottom interface are exchanged)
public
ICF = 1.2
ICF = 1.8
public

## Slide 16: Conclusions and future work
SiGe/Si/SiGe promising platform for qubits
APT can characterize the burried interfaces
Confirm accuracy with complementary technique
Apply more complex reconstruction protocol
Check effect fabrication conditions
Bring one step closer to the quantum computer
public
ICF = 1.2
ICF = 1.8
Crystallography
Density correction
ICF variation
public