## Slide 1: Revealing crystallographic information in Silicon <001> from field desorption images
Forward simulation
DEH Si 〈001〉 [8]
(detector)
[004]
Link to differences in field evaporation between modes (Field of View, surface dynamics, ...?) Further investigation!
References & Acknowledgements
[1] B. Gault et al., Miscrosc. Microanal. 12, 296 (2008)
[2] L. Yao et al., MethodsX 3, 268 (2016)
[3] A.J. Breen et al., Ultramicroscopy 243, 113640 (2023)
[4] F. De Geuser et al., Surf. Sci. 601, 536 (2007)
Overview
[5] L. Yao et al., Appl. Phys. Lett. 107, 241602 (2015)
[6] M.K. Miller and R.G. Forbes, Atom-Probe Tomography: The Local Electrode Atom Probe, Springer, New York (USA), 2014
[7] B. Gault et al., J. Appl. Phys. 105, 248 (2009)
5 um
Jeroen E. Scheerder1, Yngwie Baron2, Richard J.H. Morris1 and Claudia Fleischmann1,3
Jeroen.Scheerder@imec.be
1 imec, Kapeldreef 75, 3001, Leuven, Belgium
2 Department of Applied Physics and Science Education, Eindhoven University of Technology, Eindhoven 5612 AZ, The Netherlands
3 KU Leuven, Department of Physics and Astronomy, Quantum Solid-State Physics, B-3001 Leuven, Belgium
Crystallographic information in APT data can be used to calibrate reconstruction parameters [1]
Accurate reconstruction desirable in semiconductor technology, e.g. for dopant profiling or interface characterization with sub-nm accuracy
Pole and zone lines often readily available in metallic samples from density hit map, but not in semiconductor samples
Various metrics correlated with crystallography (multihits, charge state ratio,...) have been explored to reveal crystallographic information in APT data [2,3]
Success depends on material and experimental parameters (underlying mechanisms not fully understood yet)
Sb doped Si (Cameca PSM), 20x106 hits acquired on LEAP 5000 XR
base temperature = 50K, Voltage mode PF=20%,
KDR=0.002 ions/pulse (1/KDR~ 500)
Detector event histogram (DEH) filters based on the number of pulses between consecutive hits to reveal poles in Si<001>
novel filter, based on the relative amount of events with limited pulses in between, reveals the <311> family and other 4-fold symmetric features, for datasets containing ⪆ 2x106 hits
Practical application: reduction of detector fill with increasing tip-local electrode distance is not caused by changes in image compression, but is a “shadowing effect”
The exact origin of the revealed 4-fold symmetric crystallographic patterns (and significant differences between laser and voltage mode) requires further clarification.
Poisson (random) [4] P(Np)=KDRexp(-NpKDR)
Np histogram
Not random: at small Np, evaporation events correlated in time
Not random: at small Np, evaporation events correlated in space
Hit distance between small Np
Correlated events ~ crystallography
Stochastic evaporation
events: peak at ½ detector fill (approx. 15 mm in this case)
[4]
At low index poles [5] (center of atomic terrace): atoms subject to higher electric field F while having lower evaporation field Fe
which
decreases Np at these locations!
Possible mechanism:
Filter APT data in detector space based on Np to reveal obscured crystallographic information
(DEH)
Spatial distribution maps (aSi = 0.543 nm d004 = 0.136 nm d311= 0.164 nm)
Filtering based on number of pulses between consecutive hits Np for Si
[004]
[2,3]
Density on DEH Nhit(x,y),
Only reveals center [004] pole in silicon
Filter 0 ≤ Np ≤ 10
Only showing correlated events per pixel Np<10(x,y)
does not reveal much?
B
A
[2,3]
Novel filter: Np<10(x,y)/Nhit(x,y) (divide panel B by panel A)
Reveals novel poles (<311> family) and other 4-fold symmetric features!
[8] Y.-T. Ling et al., Microsc. Microanal. 4, 1102 (2022)
We thank M.Sc. Viktor de Ridder for part of the data acquisition, and prof. A. Vantomme (KUL) and
prof. P. Koenraad (TU/e) for fruitful discussions
Contact
Voltage mode (PF 20%)
Laser mode (2 pJ)
Interpretation?
Percentage of hits 0 ≤ Np ≤ 10
Average Np between events
0.30
0.30
[004]
Filters applied to laser mode data reveal different 4-fold symmetric features than in voltage mode
Double line / square feature
near centre pole, reminiscent of forward simulations?
Application: image formation
detector
fill
distance [004]-[311]
increase in tip-LE distance [mm]
0 mm
6 mm
12 mm
tip
local electrode(LE)
detector
detector fill
[6]
2x106 hits acquired
Voltage mode PF=20%.
Goal: understand effect of tip-local electrode distance on image formation in our system
5x106 hits acquired
With increasing tip-LE distance, detector fill decreases, while distance between poles remains constant within uncertainty.
This suggests limited change in image magnification and compression, and thus the shrinking detector fill is a result from the local electrode ‘shadowing’ the signal. (in agreement with [7])
detector fill (radius)
distance [004]-[311]
In this work: